# JSL-501 Blinking Series

# (5mm round blinking LED diode)

Features:

1.Standard brightness.

2. General application for indication

3.IC compatible /Low current capability        .

4.Long life solid state reliability.

5. RoHs compliant.

Electrical and optical characteristics(Ta=25゜с)

| ### Part Number | Dice material And color | Lens color | ### Peak Wavelength | Pulse Rate (Hz) Typ | Vf(V) Typ | Iv(mcd) |  |  | Viewing Angle TT2 θ 1/2TT |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Min | Typ | Max |  |
| JSL-501RD-B6.8 | GaAlAs/Red | Red Diffused | 625nm | 6.8Hz | 2.5-3.5 | 100 | 200 | 250 | 40° |
| JSL-501GD-B6.8 | GaP/Green | Green Diffused | 570nm | 6.8Hz | 2.5-3.5 | 10 | 20 | 30 | 40° |
| JSL-501YD-B6.8 | GaAsP/Yellow | Yellow Diffused | 589nm | 6.8Hz | 2.5-3.5 | 100 | 200 | 250 | 40° |
| JSL-501RC-B6.8 | GaAlAs/Red | Water Clear | 625nm | 6.8Hz | 2.5-3.5 | 700 | 1300 | 1800 | 25° |
| JSL-501GC-B6.8 | GaP/Green | Water Clear | 570nm | 6.8Hz | 2.5-3.5 | 70 | 100 | 120 | 25° |
| JSL-501YC-B6.8 | GaAsP/Yellow | Water Clear | 589nm | 6.8Hz | 2.5-3.5 | 700 | 1300 | 1800 | 25° |
| JSL-501BC-B6.8 | InGaN/Blue | Water Clear | 465nm | 6.8Hz | 3.5-4.5 | 1000 | 1500 | 2000 | 25° |
| JSL-501PGC-B6.8 | InGaN/Pure Green | Water Clear | 520nm | 6.8Hz | 3.5-4.5 | 2000 | 2500 | 3500 | 25° |
| JSL-501UW-B6.8 | InGan/Ultra White | Water Clear | 6000K | 6.8Hz | 3.5-4.5 | 3000 | 4000 | 5000 | 25° |

# JSL-501 Blinking Series

Absolute Maximum Ratings at Ta=25℃

| # Parameter | # Symbol | UR | UY | UG | UA | UB | BG | PG | UV | UP | UW | WW | # Unit |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Forward Current | IBBFBB | 25 | 25 | 25 | 25 | 30 | 30 | 30 | 30 | 30 | 30 | 30 | mA |
| Power Dissipation | PBBdBB | 60 | 60 | 60 | 60 | 100 | 100 | 100 | 100 | 100 | 100 | 100 | mW |
| Reverse Voltage | VBBRBB | 5 |  |  |  |  |  |  |  |  |  |  | V |
| Peak Forward Current (Duty 1/10 @1KHZ) | IBBPFBB | 150 |  |  |  |  |  |  |  |  |  |  | mA |
| Operation Temperature | TBBOPRBB | -40 to +80 |  |  |  |  |  |  |  |  |  |  | ℃ |
| Storage Temperature | TBBSTGBB | -40 to +85 |  |  |  |  |  |  |  |  |  |  | ℃ |

Package configuration:

1.All dimensions are millimeters (inches)

2.Tolerance is ±0.25mm(.010”) unless otherwise noted.