| 产品承认书 ## PRODUCT APPROVED （CUSTOMERS） # （CUSTOMER P/N） （PART NUMBER） JSS-3922Bxx （DESCRIPTION） 0.39 inch common anode 2 digits smd display （SAMPLE DATE） |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Specification |  | ### INSPECTION |  | SAMPLE |  | OTHERS |  |
| （APPROVED BY） |  | （CHECKED BY） |  | (PROOFREAD BY) |  | （PREPARED BY） |  |
| Version | Date |  | Description |  |  |  | Maker |
| （CUSTOMER VERDICT） |  |  |  |  |  |  |  |
| (OK) |  |  |  |  | (NG) |  |  |
| (APPROVED BY)： (APPROVED DATE)： |  |  |  |  |  |  |  |
| (IMPROVED ADVICE)： |  |  |  |  |  |  |  |

REMARK：FOR OFFERING THE BEST SERVICE TO CUSTOMER, PLEASE FAX THE DATA TO FACTORY

IN TIME

1.DESCRIPTION：

- Gray face，White Epoxy

- Common Anode

- Various Emiting ColorColor

- RoHS Compliant

2.FEATURES：

- High intensity and reliability

- High quality, Low power requirement

- IC compatible , Easy assembly

- ESD1000V

- 3.PACKAGE DIMENSION：

NOTES: All dimensions are in millimeters (inches) tolerance are 0.25mm(0.010) unless otherwise noted

- 4.INTERNAL CIRCUIT DIAGRAM

5.ABSOLUTE MAXIMUM RATINGS AT Ta=25C：

| Items | Symbol | Absolute maximum Rating | Unit |
| --- | --- | --- | --- |
| Forward Current(DC) | IF | 20 | mA |
| Power Dissipation | W | 60 | Mw |
| Peak Forward Current* | IFP | 100 | mA |
| Reverse Voltage | VR | 5 | V |
| Operation Temperature | Topr | -40+85 | ºC |
| Storage Temperature | Tstg | -40+100 | ºC |
| Lead Soldering Temperature | Tsol | Max .260 ℃ for 3 sec Max. (3mm from the base of the epoxy bulb) |  |

6.ELECTRICAL/OPTICAL CHARACTERISTICS AT Ta=25C：

| Part No | Emitting Color | Chip Material | Forward Voltage ( V) |  | Luminous Intensity (mcd) |  | Peak Wave Length(λP) nm |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | IF=10mA |  |  |  |  |  |
| Common Anode |  |  | Typ | Max | Min | Typ | Typ | Max |
| JSS-3922BUR-21 | Ultra Red | AlGaInP | 2.0 | 2.5 | 20 | 40 | 630 | 640 |
| JSS-3922BSR-21 | Super Red | AlGaInP | 2.0 | 2.5 | 40 | 80 | 620 | 625 |
| JSS-3922BUY-21 | Yellow | AlGaInP | 2.0 | 2.5 | 40 | 60 | 585 | 595 |
| JSS-3922BUG-21 | Green | AlGaInP | 2.0 | 2.5 | 10 | 20 | 570 | 575 |
| JSS-3922BUA-21 | Amber | AlGaInP | 2.0 | 2.5 | 40 | 60 | 600 | 610 |
| JSS-3922BUB-21 | Blue | lnGan | 3.0 | 3.5 | 40 | 60 | 460 | 470 |
| JSS-3922BPG-21 | Pure Green | lnGan | 3.0 | 3.5 | 80 | 150 | 520 | 525 |
| JSS-3922BUW-21 | White | lnGan | 3.0 | 3.5 | 100 | 200 | X0.30/Y0.30 |  |

7.Recommended Soldering Pattern：

- 推荐的SMT焊接曲线Recommended SMT condition：